## Slide 1: FWT ROLLING UPDATE 09.03.2022 CG GS

## Slide 2
FWT1030
DESMEAR DOE 2x, 1x, 0x
FIRST RESULTS

## Slide 3: FWT1030

## Slide 4: FWT1030 Mat R1551W, R1566W
MEAN STD = 236 µOHM
MEAN NO DESMEAR = 3546 µOHM
MEAN 50%STD = 252 µOHM

## Slide 5
FWT0050 – FWT0102 FIRST RESULTS

## Slide 6
FWT0050 – FWT0102 FIRST RESULTS
Currently in Production
3840 FWTµvias
Front & Back
SENSE + SENSE -
FORCE + FORCE -
S+
S-
F-
F+
S+
F+
F-
S-
S+
F+
F-
S-
S+
F+
F-
S-
S+
F+
F-
S-

## Slide 7
FWT0050 – FWT0102 FIRST RESULTS
FWT0050
FWT0100
FWT0102
FWT0101
FWT0101

## Slide 8
FWT DESIGN FOR PTH (DESMEAR)

## Slide 9
FRONT L2 L3 L4 L5 BACK
FWT DESIGN FOR PTH (DESMEAR)

## Slide 10
FWT DESIGN FOR PTH (DESMEAR)
0,2mm 0,28mm 0,6mm 1,0mm
35µm
18µm
IP copper 18µm show higher resistance values than IP Copper 35µm
0,2mm 0,28mm 0,6mm 1,0mm

## Slide 11: FWT Coupon Project WGS
Christian Galler, Gerhard Stubenberger
November 16, 2021
Quality Management, Department
Wideband Global SATCOM

## Slide 12
SCHNITT A-A
ZIC1
ZIC2
ZIC3
ZIC4
ZIC1
ZIC2
ZIC3
ZIC4
FWT-Coupon ZIC

## Slide 13
COUPON SIZE: 42,5x6mm
ZIC Coupon Positions

## Slide 14
FWT COUPONS

## Slide 15: Thank You for your attention